TEST 1

SKPN 4123 NUCLEAR REACTOR MATERIALS

2nd NOVEMBER 2015

Question 1

Define and explain the following: (10 marks)

- Frenkel pair

- Collision cascade

- Post weld heat treatment

- Intergranular stress corrosion cracking

- Chromium depletion during irradiation induced segregation(RIS)

Question 2

Based on a suitable nuclear reactor material, state and discuss the 3 factors that govern stress corrosion cracking (SCC) (6 marks)

Question 3

The presence of uncontrollable hydrogen amount in nuclear reactor can initiate hydrogen embrittlement and swelling of the nuclear metals.

- Name 3 possible sources of hydrogen in nuclear reactor (3 marks)

- Describe the phenomenon of hydrogen embrittlement and its impact (3 marks)

Question 4

- Lithium hydroxide is used in nuclear power engineering as an additive in primary coolant of PWR to maintain the water chemistry.

- Why is the addition of LiOH necessary? (2 marks)

b)   Lithium-7, instead of Lithium-6 is used for this purpose. Explain why. (2 marks)

- How does lithium Li-7 affect the susceptibility to primary water stress corrosion cracking (PWSCC)? (4 marks)

Question 5

Flow accelerated corrosion (FAC) is one the most common problems in nuclear power plants.

- Explain the FAC phenomenon and mechanisms (4 marks)

- Summarize the effect of the following parameters on the rate of FAC (5 marks)

| Parameters | Effect on FAC |
| --- | --- |
| Flow velocity |  |
| Temperature |  |
| pH |  |
| Chromium content |  |
| Dissolved oxygen |  |

- Suggest 1 approach to mitigate FAC (1 mark)