SULIT (CONFIDENTIAL)

Faculty of Chemical and Energy Engineering

FINAL EXAMINATION SEMESTER 1

SESSION 2017/2018

COURSE CODE	: 	SKPN 4123

COURSE	: 	NUCLEAR REACTOR MATERIALS

PROGRAMME	:	Bachelor of Engineering (Nuclear)

TIME	:	3 HOURS

DATE	:	14th January 2018

INSTRUCTIONS TO STUDENT:

        - Answer all questions in the answer booklet provided.

        - Students are not allowed to bring any reference materials in the examination hall.

        - Students are allowed to use scientific calculator (if necessary).

        - Students are not allowed to refer to any electronic devices such as smart handphone  etc.

CHEATING  IS STRICTLY PROHIBITED DURING EXAMINATION

________________________________________________________________________________

THIS EXAMINATION PAPER CONSISTS OF 6  PRINTED PAGES INCLUSIVE OF THIS PAGE

Question 1 (10 marks)

| C01 |  |  |
| --- | --- | --- |
| (a) | (b) | (c) |
| 4 | 2 | 4 |

- Determine the density of BCC iron, which has a lattice parameter of 0.2866 nm. 
(Atomic mass = 55.847 g/mol, Avogadro’s constant  NA=6.022 ×1023 atoms/mol)

(4 marks)

- Why is there a slight difference with the measured density of 7.870 gm/cm3 for BCC iron?

(2 marks)

- In materials, atoms are bonded either by primary or secondary bonds. List the different types of these bonds.

(4 marks)

Question 2 (30 marks)

| C02 |  |  |  |
| --- | --- | --- | --- |
| (a) | (b) | (c) | (d) |
| 3 | 10 | 10 | 7 |

- List the three most commonly used material in a nuclear reactor

(3 marks)

- List and explain five types of effects of radiation on materials.

(10 marks)

- Explain five types of damages that fission products can do to a material.

(10 marks)

- Discuss the challenges and issues concerning reactor materials with the current trend of extending the lifetime of current reactors.

(7 marks)

Question 3 (30 marks)

| C03 |  |  |  |
| --- | --- | --- | --- |
| (a) | (b) | (c) | (d) |
| 11 | 9 | 6 | 4 |

- Stress corrosion cracking (SCC) is the most prominent phenomenon that causes nuclear reactor materials degradation

  - With the help of a diagram, state the three factors that cause SCC and show how they interact with each other

(5 marks)

  - Provide and explain one example for each factor

(6 marks)

- Controlling water chemistry is important in a BWR

  - Discuss the importance of water purity in BWR and how different impurities are formed and interact, affecting reactor materials

(6 marks)

  - Should we achieve 100% purity of water? Explain your answer.

(3 marks)

- Explain one method in mitigating SCC and its limitations.

(6 marks)

- Explain two repairs/maintenance techniques for SCC in a BWR’s recirculation piping

(4 marks)

Question 4 (25 marks)

| C04 |  |  |  |
| --- | --- | --- | --- |
| (a) | (b) | (c) | (d) |
| 6 | 9 | 6 | 4 |

- Fuel material behavior is an important issue in a reactor

  - What are the functions of fuel pellets?

(1 mark)

  - What is the purpose of understanding fuel behavior?

(1 mark)

  - List four factors that interact to affect fuel behavior.

(4 marks)

- Pellet-cladding mechanical interaction is an important subject to maintain the integrity of the fuel rod.

  - Sketch a diagram showing a vertical cross-section of a fresh fuel rod, labeling all the important features.

(2 marks)

  - Redo the sketch above for a degraded fuel rod, showing and labeling all the important degradation phenomena.

(7 marks)

- Explain how burnup and irradiation degrade fuel pellet and how it affect fuel thermal behavior.

(6 marks)

- What are the desirable characteristics of cladding material? Explain one disadvantage of Zircaloy during LOCA.

(4 marks)

Question 5 (5 marks)

| C05 |  |
| --- | --- |
| (a) | (b) |
| 2 | 3 |

- In-service inspection is important to detect corrosion and cracks during operation of a power plant. List and explain the requirements of in-service inspection methods and apparatus.

(2 marks)

- Explain the three main interconnected thrust areas of the real-time monitoring approach for material degradation.

(3 marks)