## Slide 1: SKTN 2123 Strength of Materials Mechanical Properties of Materials
Mohsin Mohd Sies
Nuclear Engineering,
School of Chemical and Energy Engineering,
Universiti Teknologi Malaysia

## Slide 2: CHAPTER OBJECTIVES
Show relationship of stress and strain using experimental methods to determine stress-strain diagram of a specific material
Discuss the behavior described in the diagram for commonly used engineering materials
Discuss the mechanical properties and other test related to the development of mechanics of materials

## Slide 3: CHAPTER OUTLINE
Tension and Compression Test
Stress-Strain Diagram
Stress-Strain Behavior of Ductile and Brittle Materials
Hooke’s Law
Strain Energy
Poission’s Ratio
Shear Stress-Strain Diagram
Failure of Materials Due to Creep and Fatigue

## Slide 4: 3.1 TENSION & COMPRESSION TEST
Strength of a material can only be determined by experiment
One test used by engineers is the tension or compression test
This test is used primarily to determine the relationship between the average normal stress and average normal strain in common engineering materials, such as metals, ceramics, polymers and composites

## Slide 6: 3.1 TENSION & COMPRESSION TEST
Performing the tension or compression test
Specimen of material is made into “standard” shape and size
Before testing, 2 small punch marks identified along specimen’s length
Measurements are taken of both specimen’s initial x-sectional area A0 and gauge-length distance L0; between the two marks
Seat the specimen into a testing machine shown below.

## Slide 7: 3.1 TENSION & COMPRESSION TEST
Performing the tension or compression test
Seat the specimen into a testing machine shown below
The machine will stretch specimen at slow constant rate until breaking point
At frequent intervals during test, data is recorded of the applied load P.

## Slide 8: 3.1 TENSION & COMPRESSION TEST
Performing the tension or compression test
Elongation δ = L − L0 is measured using either a caliper or an extensometer
δ is used to calculate the normal strain in the specimen
Sometimes, strain can also be read directly using an electrical-resistance strain gauge (strain rosette)

## Slide 9: 3.2 STRESS-STRAIN DIAGRAM
A stress-strain diagram is obtained by plotting the various values of the stress and corresponding strain in the specimen
Conventional stress-strain diagram
Using recorded data, we can determine nominal or engineering stress by
P
A0
σ =
Assumption: Stress is constant over the x-section and throughout region between gauge points

## Slide 10: 3.2 STRESS-STRAIN DIAGRAM
Conventional Stress-Strain Diagram
Likewise, nominal or engineering strain is found directly from strain gauge reading, or by
δ
L0
 =
Assumption: Strain is constant throughout region between gauge points
By plotting σ (ordinate) against  (abscissa), we get a conventional stress-strain diagram

## Slide 11: 3.2 STRESS-STRAIN DIAGRAM
Conventional stress-strain diagram
Figure shows the characteristic stress-strain diagram for steel, a commonly used material for structural members and mechanical elements

## Slide 12: 3.2 STRESS-STRAIN DIAGRAM
Conventional stress-strain diagram
Elastic behavior.
A straight line
Stress is proportional to strain, i.e., linearly elastic
Upper stress limit, or proportional limit; σpl
If load is removed upon reaching elastic limit, specimen will return to its original shape

## Slide 13: 3.2 STRESS-STRAIN DIAGRAM
Conventional stress-strain diagram
Figure 3-4
Yielding.
Material deforms permanently; yielding; plastic deformation
Yield stress, σY
Once yield point reached, specimen continues to elongate (strain) without any increase in load
Note figure not drawn to scale, otherwise induced strains is 10-40 times larger than in elastic limit
Material is referred to as being perfectly plastic

## Slide 14: 3.2 STRESS-STRAIN DIAGRAM
Conventional stress-strain diagram
Figure 3-4
Strain hardening.
Ultimate stress, σu
While specimen is elongating, its x-sectional area will decrease
Decrease in area is fairly uniform over entire gauge length

## Slide 15: 3.2 STRESS-STRAIN DIAGRAM
Conventional stress-strain diagram
Figure 3-4
Necking.
At ultimate stress, x-sectional area begins to decrease in a localized region
As a result, a constriction or “neck” tends to form in this region as specimen elongates further
Specimen finally breaks at fracture stress, σf

## Slide 16: 3.2 STRESS-STRAIN DIAGRAM
Conventional stress-strain diagram
Figure 3-4
Necking.
Specimen finally breaks at fracture stress, σf

## Slide 17: 3.2 STRESS-STRAIN DIAGRAM
True stress-strain diagram
Instead of using original cross-sectional area and length, we can use the actual cross-sectional area and length at the instant the load is measured
Values of stress and strain thus calculated are called true stress and true strain, and a plot of their values is the true stress-strain diagram

## Slide 19: 3.2 STRESS-STRAIN DIAGRAM
True stress-strain diagram
In strain-hardening range, conventional σ- diagram shows specimen supporting decreasing load
While true σ- diagram shows material to be sustaining increasing stress

## Slide 20: 3.2 STRESS-STRAIN DIAGRAM
True stress-strain diagram
Although both diagrams are different, most engineering design is done within elastic range provided
  Material is “stiff,” like most metals
  Strain to elastic limit remains small
  Error in using engineering values of σ and  is very small (0.1 %) compared to true values

## Slide 21: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS
Ductile materials
Defined as any material that can be subjected to large strains before it ruptures, e.g., mild steel
Such materials are used because it is capable of absorbing shock or energy, and if before becoming overloaded, will exhibit large deformation before failing
Ductility of material is to report its percent elongation or percent reduction in area at time of fracture

## Slide 22: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS
Ductile materials
Percent elongation is the specimen’s fracture strain expressed as a percent
Percent reduction in area is defined within necking region as
Percent elongation =
Lf − L0
L0
(100%)
Percent reduction in area =
A0 − Af
A0
(100%)

## Slide 23: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS
Ductile materials
Most metals do not exhibit constant yielding behavior beyond the elastic range, e.g. aluminum
It does not have well-defined yield point, thus it is standard practice to define its yield strength using a graphical procedure called the offset method

## Slide 24: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS
Ductile materials
Offset method to determine yield strength
Normally, a 0.2 % strain is chosen.
From this point on the  axis, a line parallel to initial straight-line portion of stress-strain diagram is drawn.
The point where this line intersects the curve defines the yield strength.

## Slide 25
3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS

## Slide 26: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS
Brittle Materials
Material that exhibit little or no yielding before failure are referred to as brittle materials, e.g., gray cast iron
Brittle materials do not have a well-defined tensile fracture stress, since appearance of initial cracks in a specimen is quite random

## Slide 27: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS
Brittle Materials
Instead, the average fracture stress from a set of observed tests is generally reported

## Slide 28: 3.3 STRESS-STRAIN BEHAVIOR OF DUCTILE & BRITTLE MATERIALS

## Slide 29: 3.4 HOOKE’S LAW
E represents the constant of proportionality, also called the modulus of elasticity or Young’s modulus
E has units of stress, i.e., pascals, MPa or GPa.
Most engineering materials exhibit a linear relationship between stress and strain with the elastic region
Discovered by Robert Hooke in 1676 using springs, known as Hooke’s law
σ = E

## Slide 30: 3.4 HOOKE’S LAW
E is a mechanical property that indicates the stiffness of a material.
Materials that are very stiff exhibits large values of E (Esteel = 200GPa.
E only valid in linear elastic behavior and no longer valid once the σ–ε diagram ceases to be a straight line

## Slide 31: 3.4 HOOKE’S LAW
As shown above, most grades of steel have same modulus of elasticity, Est = 200 GPa
Modulus of elasticity is a mechanical property that indicates the stiffness of a material
Materials that are still have large E values, while spongy materials (vulcanized rubber) have low values

## Slide 32: 3.4 HOOKE’S LAW
IMPORTANT
Modulus of elasticity E, can be used only if a material has linear-elastic behavior.
Also, if stress in material is greater than the proportional limit, the stress-strain diagram ceases to be a straight line and the equation is not valid

## Slide 33: 3.4 HOOKE’S LAW
Strain hardening
If a specimen of ductile material (steel) is loaded into the plastic region and then unloaded, elastic strain is recovered as material returns to its equilibrium state
However, plastic strain remains, thus material is subjected to a permanent set

## Slide 34: 3.4 HOOKE’S LAW
Strain hardening
Specimen loaded beyond yield point A to A’
Inter-atomic forces have to be overcome to elongate specimen elastically, these same forces pull atoms back together when load is removed
Since E is the same, slope of line O’A’ is the same as line OA.
However, upon reloading, specimen will exhibit new and higher yield strength.

## Slide 35: 3.4 HOOKE’S LAW
Strain hardening
Load reapplied, atoms will be displaced until yielding occurs at or near A’, and stress-strain diagram continues along same path as before
New stress-strain diagram has higher yield point (A’), a result of strain-hardening
Specimen has a greater elastic region and less ductility

## Slide 36: 3.4 HOOKE’S LAW
Strain hardening
As specimen is unloaded and loaded, heat or energy may be lost
Colored area between the curves represents lost energy and is called mechanical hysteresis
It’s an important consideration when selecting materials to serve as dampers for vibrating structures and equipment

## Slide 37: Hooke’s Law: Modulus of Elasticity
Below the yield stress
Strength is affected by alloying, heat treating, and manufacturing process but stiffness (Modulus of Elasticity) is not.

## Slide 38: 3.5 STRAIN ENERGY
When material is deformed by external loading, energy is stored internally throughout its volume
Internal energy is also referred to as strain energy
Stress develops a force,
F = σ A = σ (x y)

## Slide 39: 3.5 STRAIN ENERGY
Strain-energy density is strain energy per unit volume of material
u =
∆U
∆V
σ
2
=
If material behavior is linear elastic, Hooke’s law applies,
u =
σ
2
σ2
2E
=
σ

( )

## Slide 40: 3.5 STRAIN ENERGY
Modulus of resilience
When stress reaches proportional limit, strain-energy-energy density is called modulus of resilience
A material’s resilience represents its ability to absorb energy without any permanent damage
ur =
σpl pl
2
σpl2
2E
=

## Slide 41: 3.5 STRAIN ENERGY
Modulus of toughness
Modulus of toughness ut, indicates the strain-energy density of material before it fractures
Shaded area under stress-strain diagram is the modulus of toughness
Used for designing members that may be accidentally overloaded
Higher ut is preferable as distortion is noticeable before failure

## Slide 42: EXAMPLE 3.1
Tension test for a steel alloy results in the stress-strain diagram below.
Calculate the modulus of elasticity and the yield strength based on a 0.2%.

## Slide 43
Modulus of elasticity
Calculate the slope of initial straight-line portion of the graph. Use magnified curve and scale shown in light blue, line extends from O to A, with coordinates (0.0016 mm, 345 MPa)
E =
345 MPa
0.0016 mm/mm
= 215 GPa
EXAMPLE 3.1 (SOLN)

## Slide 44
Yield strength
At 0.2% strain, extrapolate line (dashed) parallel to OA till it intersects stress-strain curve at A’
σYS = 469 MPa
EXAMPLE 3.1 (SOLN)

## Slide 45
Ultimate stress
Defined at peak of graph, point B,
σu = 745.2 MPa
EXAMPLE 3.1 (SOLN)

## Slide 46
Fracture stress
When specimen strained to maximum of f = 0.23 mm/mm, fractures occur at C.
Thus,
σf = 621 MPa
EXAMPLE 3.1 (SOLN)

## Slide 50: EXAMPLE 3.3 (SOLN)
Determine the approx. Δ, of the rod when 10kN axial load is applied? Use given stress-strain diagram to calculate the permanent elongation of the rod if the load is removed.

## Slide 53: 3.6 POISSON’S RATIO
When body subjected to axial tensile force, it elongates and contracts laterally
Similarly, it will contract and its sides expand laterally when subjected to an axial compressive force

## Slide 54: 3.6 POISSON’S RATIO
Strains of the bar are:
long =
δ
L
lat =
δ’
r
Poisson’s ratio, ν = −
lat
long
Early 1800s, S.D. Poisson realized that within elastic range, ratio of the two strains is a constant value, since both are proportional.

## Slide 55: 3.6 POISSON’S RATIO
ν is unique for homogenous and isotropic material
Why negative sign? Longitudinal elongation cause lateral contraction (-ve strain) and vice versa
Lateral strain is the same in all lateral (radial) directions
Note that, no force or stress acts in a lateral direction in order to strain the material; the strain is caused only by axial force.
Poisson’s ratio is dimensionless, 0 ≤ ν ≤ 0.5

## Slide 56: EXAMPLE 3.4
Bar is made of A-36 steel and behaves elastically.
Determine change in its length and change in dimensions of its cross section after load is applied.

## Slide 57: EXAMPLE 3.4 (SOLN)
Normal stress in the bar is
σz =
P
A
= 16.0(106) Pa
From tables, Est = 200 GPa, strain in z-direction is
z =
σz
Est
= 80(10−6) mm/mm
Axial elongation of the bar is,
δz = zLz = [80(10−6)](1.5 m) = −25.6 μm/m

## Slide 58: EXAMPLE 3.4 (SOLN)
Using νst = 0.32, contraction strains in both x and y directions are
Thus changes in dimensions of cross-section are
x = y = −νstz = −0.32[80(10−6)] = −25.6 μm/m
δx = xLx = −[25.6(10−6)](0.1 m) = −25.6 μm
δy = yLy = −[25.6(10−6)](0.05 m) = −1.28 μm

## Slide 59: 3.6 SHEAR STRESS-STRAIN DIAGRAM
Use thin-tube specimens and subject it to torsional loading
If the material is homogeneous and isotropic, then the shear stress as a result of torsional loading will caused uniform distortion.
Record measurements of applied torque and resulting angle of twist to construct shear stress and shear strain diagram.

## Slide 60: 3.6 SHEAR STRESS-STRAIN DIAGRAM
Material will exhibit linear-elastic behavior till its proportional limit, τpl
Strain-hardening continues till it reaches ultimate shear stress, τu
Material loses shear strength till it fractures, at stress of τf

## Slide 61: 3.6 SHEAR STRESS-STRAIN DIAGRAM
Hooke’s law for shear
τ = Gγ
G is shear modulus of elasticity or modulus of rigidity
G can be measured as slope of line on τ-γ diagram, G = τpl/ γpl
The three material constants E, ν, and G is related by
G =
E
2(1 + ν)

## Slide 62: EXAMPLE 3.5
Specimen of titanium alloy tested in torsion & shear stress-strain diagram shown below.
Determine shear modulus G, proportional limit, and ultimate shear stress.
Also, determine the maximum distance d that the top of the block shown, could be displaced horizontally if material behaves elastically when acted upon by V. Find magnitude of V necessary to cause this displacement.

## Slide 63: EXAMPLE 3.5 (SOLN)
Shear modulus
Obtained from the slope of the straight-line portion OA of the τ-γ diagram. Coordinates of A are (0.008 rad, 360 MPa)
G =
= 45(103) MPa
360 MPa
0.008 rad

## Slide 64: EXAMPLE 3.5 (SOLN)
Proportional limit
By inspection, graph ceases to be linear at point A, thus,
τpl = 360 MPa
Ultimate stress
From graph,
τu = 504 MPa

## Slide 65: EXAMPLE 3.5 (SOLN)
Maximum elastic displacement and shear force
By inspection, graph ceases to be linear at point A, thus,
tan (0.008 rad) ≈ 0.008 rad =
d
50 mm
d = 0.4 mm
τavg =
V
A
360 MPa =
V
(75 mm)(100 mm)
V = 2700 kN

## Slide 66: EXAMPLE 3.6 (SOLN)

## Slide 67: EXAMPLE 3.6 (SOLN)

## Slide 68: 3.7 FAILURE OF MATERIALS DUE TO CREEP & FATIGUE
Creep
Occurs when material supports a load for very long period of time, and continues to deform until a sudden fracture or usefulness is impaired
Is only considered when metals and ceramics are used for structural members or mechanical parts subjected to high temperatures
Other materials (such as polymers & composites) are also affected by creep without influence of temperature

## Slide 69: *3.7 FAILURE OF MATERIALS DUE TO CREEP & FATIGUE
Creep
Stress and/or temperature significantly affects the rate of creep of a material
Creep strength represents the highest initial stress the material can withstand during given time without causing specified creep strain
Simple method to determine creep strength
Test several specimens simultaneously
  At constant temperature, but
  Each specimen subjected to different axial stress

## Slide 70: *3.7 FAILURE OF MATERIALS DUE TO CREEP & FATIGUE
Creep
Simple method to determine creep strength
Measure time taken to produce allowable strain or rupture strain for each specimen
Plot stress vs. strain
Creep strength inversely proportional to temperature and applied stresses

## Slide 71: *3.7 FAILURE OF MATERIALS DUE TO CREEP & FATIGUE
Fatigue
Defined as gradual deterioration of a material that is subjected to time varying loads.
Needs to be accounted for in design of connecting rods (e.g. steam/gas turbine blades, connections/supports for bridges, railroad wheels/axles and parts subjected to cyclic loading)
Fatigue occurs at a stress lesser than the material’s yield stress

## Slide 72: *3.7 FAILURE OF MATERIALS DUE TO CREEP & FATIGUE
Fatigue
Also referred to as the endurance or fatigue limit
Method to get value of fatigue
Series of specimens are subjected to a specified stress and cycled to failure.
Plot stress (S) against number of cycles-to-failure N (S-N diagram) on logarithmic scale – also known as stress-cycled diagram.

## Slide 73: CHAPTER REVIEW
Tension test is the most important test for determining material strengths. Results of normal stress and normal strain can then be plotted.
Many engineering materials behave in a linear-elastic manner, where stress is proportional to strain, defined by Hooke’s law, σ = E. E is the modulus of elasticity, and is measured from slope of a stress-strain diagram
When material stressed beyond yield point, permanent deformation will occur.

## Slide 74: CHAPTER REVIEW
Strain hardening causes further yielding of material with increasing stress
At ultimate stress, localized region on specimen begin to constrict, and starts “necking”. Fracture occurs.
Ductile materials exhibit both plastic and elastic behavior. Ductility specified by permanent elongation to failure or by the permanent reduction in cross-sectional area
Brittle materials exhibit little or no yielding before failure

## Slide 75: CHAPTER REVIEW
Yield point for material can be increased by strain hardening, by applying load great enough to cause increase in stress causing yielding, then releasing the load. The larger stress produced becomes the new yield point for the material
Deformations of material under load causes strain energy to be stored. Strain energy per unit volume/strain energy density is equivalent to area under stress-strain curve.

## Slide 76: CHAPTER REVIEW
The area up to the yield point of stress-strain diagram is referred to as the modulus of resilience
The entire area under the stress-strain diagram is referred to as the modulus of toughness
Poisson’s ratio (ν), a dimensionless property that measures the lateral strain to the longitudinal strain [0 ≤ ν ≤ 0.5]
For shear stress vs. strain diagram: within elastic region, τ = Gγ, where G is the shearing modulus, found from the slope of the line within elastic region

## Slide 77: CHAPTER REVIEW
G can also be obtained from the relationship of G = E/[2(1+ ν)]
When materials are in service for long periods of time, creep and fatigue are important.
Creep is the time rate of deformation, which occurs at high stress and/or high temperature. Design the material not to exceed a predetermined stress called the creep strength

## Slide 78: CHAPTER REVIEW
Fatigue occur when material undergoes a large number of cycles of loading. Will cause micro-cracks to occur and lead to brittle failure.
Stress in material must not exceed specified endurance or fatigue limit